KARAKTERISASI BIODIESEL DARI MINYAK JELANTAH

HASIL FISISORPSI ZEOLIT ALAM TERAKTIVASI

Abstrak

Telah dilakukan penelitian untuk menganalisa pengaruh penggunaan zeolit alam yang telah diaktivasi sebagai penyerap (adsorben) pada minyak jelantah untuk bahan pembuatan biodiesel dengan kualitas biodiesel yang dihasilkan dari hasil fisisorpsi zeolit alam teraktivasi tersebut. Sampel biodiesel yang digunakan yaitu biodiesel TZ (Tanpa Zeolit) yang dibuat dari minyak jelantah tanpa menggunakan zeolit alam sebagai adsorben, biodiesel TA (Tanpa Aktivasi)  yang menggunakan zeolit alam sebagai adsorben namun tanpa aktivasi, biodiesel A1 100 yang menggunakan zeolit alam yang telah diaktivasi selama satu jam pada temperatur 100 oC, biodiesel A2 100, A1 150, A2 150, A1 200 dan A2 200. Semua sampel dikarakterisasi dengan menggunakan uji sifat fisik yaitu kerapatan relatif, viskositas kinematik, densitas dan uji korosi terhadap lempeng tembaga yang sesuai standar ASTM dan Dirjen Migas, serta menggunakan uji kualitatif GC-MS. Hasil penelitian menunjukkan bahwa zeolit alam yang telah diaktivasi secara fisika terbukti mampu meningkatkan kualitas biodiesel dari minyak jelantah. Waktu dan temperatur aktivasi zeolit alam secara fisika berpengaruh terhadap kualitas biodiesel yang menggambarkan kemampuan zeolit alam dalam melakukan fisisorpsi terhadap minyak jelantah. Hasil karakterisasi sifat fisik biodiesel maupun uji kualitatif GC-MS memperlihatkan bahwa biodiesel yang memenuhi standar untuk semua pengujian adalah A2 150, A1 200 dan A2 200.

Kata kunci: Biodiesel, Zeolit alam, Minyak Jelantah

CHARACTERIZATION OF BIODIESEL FROM USED COOKING OIL 
RESULTS OF FISISORPTION  BY ACTIVATED NATURAL ZEOLITE 

Abstract

This Research have been done in order to analyze the relationship between the using activated natural zeolite as adsorbent material in the manufacture of biodiesel from used cooking oil with the purpose of biodiesel quality produced by fisisorption of activated natural zeolite. Samples of biodiesel used is biodiesel TZ that made from used cooking oil without using natural zeolite as an adsorbent, biodiesel TA which uses natural zeolite as an adsorbent but without activation, biodiesel A1 100 which uses natural zeolite is activated for one hour at temperature of 100 0C, biodiesel A2 100, A1 150, A2 150, A1 200 and A2 200. All samples were characterized using an appropriate test of the physical properties such as specific gravity, viscosity kinematic, density, and copper strip corrosion of ASTM standards and the Director General of Oil and Gas, as well as a qualitative test using GC-MS. The results showed that activated natural zeolites by physics proved able to improve the quality of biodiesel from used cooking oil. Time and temperature activation of natural zeolite in physics affects the quality of biodiesel, in this case show a relationship of time and temperature activation of natural zeolite is directly proportional to the ability of natural zeolite in doing fisisorption of used cooking oil. The results of characterization of physical properties of biodiesel and qualitative test GC-MS showed that the biodiesel that meets the standards for all test is A2 150, A1 200 and A2 200.

Key words: Biodiesel, Natural Zeolite, Used Cooking Oil